## Slide 1: Hairpins Laser Welding
A suitable technology for improved efficiency
Contents at a glance
Our equipment
Stripping and Welding processes

## Slide 2
TruDisk_5001 from Trumpf :
  A solid-disc laser machine
  BrightLine Weld Technology
  VisionLine control system
  Programmable PFO Optics : PFO 33
  Power : 120 – 5000 W
  Wave length : 1030 nm
  Beam quality : 4 mm.mrad
  Focal distance : 239,5 mm
TECHNAX machine installation :
  3 digital axes
  Confined and secure enclosure
  Pneumatic inert gas circuit
Example of TECHNAX tools (Hairpin):
    A Stripping position
    A Welding position
Our Industrial Laser Machine

## Slide 3
Stripping process
25.11.2020
3
Test parts (enamelled copper terminals) are cut on a template
2. Ends of these parts are flattened
3. One part is placed in the tool
4. First mechanical adjustement stop is calibrated
5. Tool is placed on the holding table
6. Height of the Pin is adjusted by the second stop
7. Tool is placed in Stripping position
8. Digital axes are adjusted relative to the position of the Pin
9. Pneumatic circuit and the laser are switched on
10. When the laser is initialized, the laser stripping program starts
11. Same process is repeated for the other side of the part (Step 4)
13. Finally, part stripped sides are cleaned with ethanol
12. Second part is stripped following the same procedure

## Slide 4
Stripping process
Laser stripping Program parameters
Power : 275 W – 100% ring
Duration of the process for one side : 953 ms
Energy consumption : 25,69 J

## Slide 5
Welding process
1. Both stripped parts are placed in the holding tool
2. First mechanical adjustement stop is calibrated
3. Tool is put on the holding table
4. Height of the Pins is adjusted by the second stop
5. Tool is loaded in welding position
6. The digital axes are adjusted relative to the position of the Pins
7. The pneumatic circuit and the laser are switched
8. After machine initialization, the laser welding program starts

## Slide 6
Welding process
Laser welding Program parameters
Power : 3500 W – 100% heart
Duration of the process : 298 ms
Energy consumption : 40,19 J